## Slide 1: Electric charge limits on settled powders
CHISA 2016, Prague (Czech Republic)
Dept. of Electronics and Electromagnetism, Faculty of Physics, University of Seville, Spain.
Project leader (PH.D. director): M.A.S. Quintanilla.
IFPRI Ph.D. student: J. Pérez-Vaquero.

## Slide 2: Contents.
# Introduction
- Basic theory, charge transfer models.
# Experimental setup
# Results
- Charge in suspended particles.
- Charge in settled particles.
- Particle charge distributions.
- Charge layer model.
# Conclusions
J.Pérez-Vaquero, M.A.S. Quintanilla, A. Castellanos, Journal of Applied Physics 119, 223302(2016)

## Slide 3: Introduction.
Tribocharging or frictional charging is the process whereby a net electric charge emerge after the contact of two solid surfaces. Different energy levels in the contacting materials give rise to a transfer of electric charge from one surface to the other, thus breaking the initial charge balance in the system.

## Slide 4: Introduction.
E can be very high for small gaps, r <<.
Back transfer limits the maximum surface charge. It triggers when 3 x 106 V/m for air.
Back transfer is lower in vacuum.
+
-
Contact/Impact
Insulator A -Insulator B
Separation
EFA
EFB
d
Metal A
Metal B
eVC
Energy
Charge carriers
Potential energy
+
-
r
q
-q
Aggregation
Surface conductivity, , leaks charge away.
Enhanced local fields, cause corona discharge to begin ( is reached).

## Slide 5: Experimental setup.
0.0000 g
I/O
Tare
A
Compressed gas
Venturi dispersion unit
Material feeding
A
Electric currents and flowing to the Faraday pail and the steel pipe are measured as a function of time.
, obtained by integration of is the electric charge acquired by the dispersed powder.
, obtained by integration of is the electric charge remaining in the settled powder.
Cornstarch.
5-50 µm glass beads.
70-110 µm glass beads.
90-150 µm glass beads.
PMMA beads.
Semoline.
Sugar.
Tested materials:

## Slide 6: Charge limits in suspended particles.
Average charge per particle in dispersion is determined from the electric current flowing to the tribocharger, the dispersed mass and the particle radius .
Blue: stored at 56% RH, dispersed in compressed air.
Red: stored at 30% RH, dispersed in compressed air.
Green: stored in dry N2, dispersed in dry N2.
Maximum charge, limited by electric field for corona discharge in air .
| |

## Slide 7: Particle charge distributions.
Particle Tracking Velocimetry (PTV) of charged 5-50 µm glass beads.
There is a bipolar charge distribution in particle charging.
After addition, the net charge is of the same polarity as that measured in the Faraday pail.
Surface charge is roughly constant with particle size for larger radii.

## Slide 8: Charge in settled powders.
Blue: stored at 56% RH, dispersed in compressed air.
Red: stored at 30% RH, dispersed in compressed air.
Green: stored in dry N2, dispersed in dry N2.
Cumulative charge in the Faraday pail and collected mass have a sublinear relation.
Newer settling powder retain lesser charge than the older.
Black: storage RH not controlled, dispersed in compressed air.
Charge to mass ratio, qmr, depends on total cumulative charge and total collected mass:

## Slide 9: Charge layer model.
It assumes an infinite powder layer in the horizontal plane, made of dielectric material.
The settled powder has a charge per unit volume, r, an electrical conductivity, s, a bulk density, rm, and a height, z.
The incoming powder layer has a charge, ro, and is fed at a mass rate Fm.
The bottom plate has a zero surface charge, sp, at the beginning of the experiment, that becomes non zero afterwards.
System equations:
Electrical conduction
ro
r
sp
Conductive plate

## Slide 10: Charge layer model.
Charge (adimensional)
Sublinear relation

## Slide 11: Charged layer model.
Solid line: Prediction of qmr vs collected mas for pmma beads.

## Slide 12: Conclusions.
The maximum electric charge on a particle surface in dilute suspension is limited by the breakdown field of gas rather than physical mechanisms during charge transfer.
Charge in settled powders is concentrated in the layers close to the powder surface.
Charge to mass ratio (qmr) in the powder decreases with the collected mass.
Aggregation and deposition of charged particles is accompanied by corona discharge.