## Slide 1
ABS HIPS
HDPE
TRIBO-ELECTROSTATIC SEPARATION OF MIXED GRANULAR INSULATORS
Thami ZEGHLOUL
Lucien DASCALESCU
PPRIME Institute
University of Poitiers
FRANCE

## Slide 2
Background
Tribocharging devices
Tribo-electrostatic separators
Conclusions & Perspectives
OUTLINE

## Slide 3
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
TRIBOLOGY
Charles Auguste
COULOMB
b. 1736: Angoulême
d. 1806: Paris
ELECTROSTATICS
PPRIME Institute – Angoulême Campus:
Two research units: “TRIBOLUB” – “ELSTAT”

## Slide 4
Ref. | (+) |  |  |  |  |  |  |  |  |  | (-)
Iuga et al. | Al | PMMA |  |  |  |  | PE | PET | PP | PVC | 
Diaz & Felix-Navarro | PA | PMMA | PC | PS |  |  | PE | PP | PET | PVC | PTFE
Park et al. |  | PMMA |  | PS | ABS |  | PET | PE | PP | PVC | PTFE
Park et al. |  | PMMA |  | PS | ABS | HIPS | PET | PE | PP | PVC | 
Triboelectric series
Tribo-
charging
mechanisms
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives

## Slide 5
Industrial tribo-electrostatic separators
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Hamos GmbH, Penzberg, Germany

## Slide 6
6
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Fluidized Bed Device

## Slide 7
7
PET concentrate obtained by electrostatic separation of the
90% PET & 10% PVC mixture
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Choice of device wall material

## Slide 8
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Propeller-type
device
Cyclone-type
device

## Slide 9
1: tribocharging tubes; 2: opening for the evacuation
of the charged particles; 3: slider; 4: base plate;
5: tube-carrying plate; 6: eccentric wheel;
7: driving electric motor
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Vibratory device

## Slide 10
Feeder
Upper
Frame
HV
Electrodes
Lower
Frame
Collector
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Free-fall electrostatic separator
Vibratory
tribo-
charging
device

## Slide 11
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Tribo-aero-electrostatic Separator for
Granular Plastics from WEEE
Patent
FR2943561 (2009),
WO2010109096 (2010)

## Slide 12
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Tribo-aero-electrostatic Separator for
Granular Plastics from WEEE
ABS HIPS

## Slide 13
Industrial and pilot-plant TAE separators,
designed for APR2, France
ABS HIPS
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives

## Slide 14
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Multi-modal Electrostatic Separator for
Sub-millimetric Granular Materials
Partners : INRA Montpellier, U. Tech. Cluj-Napoca, U. Sidi-Bel-Abbes

## Slide 15
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Tribo-Aero-Electrostatic Separator for
Sub-millimetric Granular Materials
Partners : CITF, APR2, INRA Montpellier, U. Sidi-Bel-Abbes

## Slide 16
Background
Tribocharging devices
Tribo-electrostatic
separators
Conclusions & Perspectives
Using of DBD to modify the surface state
of the granular plastics and
improve the efficiency of
triboelectric charging
of larger particles
Numerical modelling of the
tribo-electrostatic separation
Processes
Development of novel
applications of the
tribo-electrostatic separation

## Slide 17
17
Thank you !