## Slide 1: Measurement of electric charge in gas dispersed particles using Particle Tracking Velocimetry
Miguel Ángel Sánchez Quintanilla
Javier Pérez Vaquero
Departamento de Electrónica y Electromagnetismo, Facultad de Física, Universidad de Sevilla
Grupo de Electrohidrodinámica y Medios Granulares Cohesivos.

## Slide 2: Motivation
mJ/m2
Capilary forces.
Electric force.
Weight.
g/cm3
vdW forces
m

## Slide 3: Experimental set-up
End of steel tube tribocharger
High- intensity led
Fiberglass extension with glass window
High speed camera and magnifying optics
Compressed air
Venturi dispersion unit
Material feeding
A
LED
High speed camera
High voltage (AC)

## Slide 4: Detection algorithm
Except 5-50 µm glass beads (example, the largest sample tested), other samples appear agglomerated in the images.
Image segmentation by thresholding
Removes particles out of focus.
Background removal
Subtraction of average of all frames
Particle identification
Own code based in nearest neighbours.
Trajectory linkage
ImageJ tracking tool by Sbalzarini & KoumoutSakos
fr0
fr1
fr2
fr3
fr4
fr5
fr6
fr7
fr8
fr9
fr12
fr13
fr14
fr16
fr15
fr17
fr18
fr19
fr20

## Slide 5: Forces acting on a particle /agglomerate
Drag force opposing oscillatory motion
Force due to the electric field
Drag force opposing falling motion
Weight
Is the width of the vorticity layer due to the oscillatory motion
From Landau & Lifschizt, course of theoretical physics, vol 6, Fluid mechanics.

## Slide 6: Equations and range of validity
For the vertical motion:
For the horizontal motion:
Valid if
Valid in each of these two cases:
Case 1:
Case 2:
and
Where xo is the amplitude of oscillation
and
For f=100 Hz in air

## Slide 7: Materials
Glass beads µm
Sipernat 320DS (hydrophylic)
µm
Regolith simulant
Milled sand
Sipernat D10 (hydrophobic)
µm
Measured in Mastersizer 2000. Gas: air. Dispersion pressure 1 bar.
is surface-weighed mean diameter.





Resolution limit
Resolution limit
Resolution limit
Resolution limit
Resolution limit

## Slide 8: Relevant solutions
For the vertical motion:
For the horizontal motion:
Velocity relaxation time:
Terminal velocity:
Velocity relaxation time:
Steady-state amplitude of oscillation
Steady state phase lag with the electric field
An estimation of xo is needed to calculate the Reynolds number Rex. For that we need to know the typical charge per particle q.

## Slide 9: Average charge per particle.
Compressed air
Venturi dispersion unit
Material feeding
A
We assume the charge to mass ratio of a particle q/m is the same as that of the whole sample Q/M
We use the value of the surface-volume mean diameter for R.
The largest uncertainty comes from the value of the dispersed mass M.

## Slide 10: Average charge per particle vs. particle surface-mean diameter
Ec=30 kV/cm
Experiments with continuous flow
PTV experiments (pulsed flow)
(qd in pC, R in µm)
(qd in pC, R in µm)

## Slide 11: Check on validity for the surface volume mean diameter.
Plots for p=2.5 g/cm3 Eo=3.4 kV/cm
Reynolds number
Typical times to achieve steady state.
Using the surface-volume mean diameter both conditions are met.

## Slide 12: Relevant solutions
Amplitude of oscillation
Phase lag with the field
Markers represent values for surface-mean diameter. Experiment yield a distribution of values.
Plots for p=2.5 g/cm3 Eo=3.4 kV/cm

## Slide 13: Size determination from images
To evaluate the electric charge of each particle we need to know its radius R. Two options are possible:
Circular equivalent diameter.
Aerodynamic diameter.
Calculated from the vertical velocity vz of the particle.
Calculated from the number of pixels Np of each particle in the image.
xp = 7.4 µm/pixel is the resolution of our images
Terminal velocity assuming Stokes drag:

## Slide 14: Sizing glass beads 5-50 µm
Size distributions
Vertical velocity vs. Circular equivalent diameter.
No. of particles analyzed: 708 (goodness of fit r2>0.6)
µm, p = 2.5 g/cm3

## Slide 15: Sizing Regolith simulant
Size distributions
Vertical velocity vs. Circular equivalent diameter.
No. of particles analyzed: --- (goodness of fit r2>0.6)
µm, p=2.9 g/cm3

## Slide 16: Sizing milled sand
Size distributions
Vertical velocity vs. Circular equivalent diameter.
No. of particles analyzed: 2009 (goodness of fit r2>0.6)
µm, p = 2.5 g/cm3

## Slide 17: Sizing sipernat 320 DS
Size distributions
Vertical velocity vs. Circular equivalent diameter.
No. of particles analized: 305 (goodness of fit r2>0.6)
µm, p = 2.5 g/cm3

## Slide 18: Sizing sipernat D10
Size distributions
Vertical velocity vs. Circular equivalent diameter.
No. of particles analyzed: 3616 (goodness of fit r2>0.9)
µm, p = 2.5 g/cm3

## Slide 19: Election of the sizing procedure
For all samples, specially the ones with smaller particle size, the circular equivalent diameter measured from the images tends to overestimate the size of the particles.
PSD of the circular equivalent diameter appear shifted to larger sizes compared from PSD from Mastersizer and aerodynamic diameter.
The measured vertical velocity of the particles is always smaller than the value expected from their circular equivalent diameter.
For these reasons we use the aerodynamic radius to substitute in the calculations.

## Slide 20: Glass beads 5-50 µm
Amplitude of oscillation
Phase with respect to the field
No. of particles analyzed: 708 (goodness of fit r2>0.6)
µm, p = 2.5 g/cm3

## Slide 21: Regolith simulant
No. of particles analyzed: --- (goodness of fit r2>0.6)
µm, p=2.9 g/cm3
Amplitude of oscillation
Phase with respect to the field

## Slide 22: Milled sand
No. of particles analyzed: 2009 (goodness of fit r2>0.6)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 23: Sipernat 320DS
No. of particles analized: 305 (goodness of fit r2>0.6)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 24: Sipernat D10
No. of particles analyzed: 3616 (goodness of fit r2>0.9)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 25: Charge distributions
5-50 glass beads
All materials show a charge distribution spanning of both polarities
Sipernat 320DS (hydrophylic)
Regolith simulant
Milled sand
Sipernat D10 (hydrophobic)

## Slide 26: Overall charge distribution

## Slide 27: The following slides represent results vs. circular equivalent radius

## Slide 28: Glass beads 5-50 µm
Amplitude of oscillation
Phase with respect to the field
No. of particles analyzed: 708 (goodness of fit r2>0.6)
µm, p = 2.5 g/cm3

## Slide 29: Regolith simulant
No. of particles analyzed: --- (goodness of fit r2>0.6)
µm, p=2.9 g/cm3
Amplitude of oscillation
Phase with respect to the field

## Slide 30: Milled sand
No. of particles analyzed: 2009 (goodness of fit r2>0.6)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 31: Sipernat 320DS
No. of particles analized: 305 (goodness of fit r2>0.6)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 32: Sipernat D10
No. of particles analyzed: 3616 (goodness of fit r2>0.9)
Amplitude of oscillation
Phase with respect to the field
µm, p = 2.5 g/cm3

## Slide 33: Charge distributions
5-50 glass beads
All the data show a distribution with particles of both polarities
Sipernat 320DS (hydrophylic)
Regolith simulant
Milled sand
Sipernat D10 (hydrophobic)